## Slide 1: UNIT: Oxy-Acetylene; Welding, Brazing, Cutting and Heating
Lesson: Oxy-Fuel Torch Cutting (OFC)
Standard B7.1 – Understand the role of heat and oxidation in the cutting process.
Standard B7.3 – Know how to flame-cut metal with an oxy-fuel cutting torch.

## Slide 2: Cutting Equipment versus Welding Equipment
Oxy-Fuel gas cutting equipment is used throughout the metal-working world for cutting steel and ferrous (iron-based) metals.
The equipment is basically the same for both oxy-fuel gas cutting and oxy-fuel gas welding, except for the torch.
The cutting torch is a unique and invaluable tool that enables the operator to cut almost any thickness of steel to the required size and shape.

## Slide 3: Oxy-Fuel Cutting
Oxy-fuel gas cutting is also referred to as flame cutting.
Flame cutting is a process of cutting steel by removing material to form a slot, called the kerf.
The metal is actually removed from the kerf by burning it away.
Flame cutting is one of the fastest and most efficient methods for cutting thick metal.

## Slide 4: Elements for Burning - Fuel
To understand how metal can be cut quickly with a flame, you must first understand how burning takes place
Three essential elements are needed for burning: Fuel, Oxygen, and Heat.
Fuel can be any material that will chemically combine with oxygen.
In this case, the steel to be cut is the fuel.

## Slide 5: Elements for Burning - Oxygen
Second, a large quantity of pure oxygen is needed to combine with the fuel.
The more oxygen present, and the greater the oxygen’s force, the faster burning will take place.
Therefore, flame cutting requires a jet stream of pure oxygen directed onto the steel.

## Slide 6: Elements for Burning - Heat
Third, heat is needed to raise the temperature of the steel until it reaches its ignition temperature.
Ignition temperature is the temperature at which the material will burn when oxygen is present.
The ignition or kindling temperature of steel is 1500 degrees Fahrenheit.
At this temperature, steel turns cherry red.
The stream of oxygen is directed onto the hot metal.
The steel burns rapidly, and a slot is cut through the entire piece.
The oxygen and hot steel are actually combining to form a chemical reaction called oxidation.

## Slide 7: Flame Cutting – How it works?
The Oxy-Fuel cutting process is accomplished by bringing the base metal to a molten state, then introducing a high-pressure stream of cutting oxygen.

## Slide 8: Flame Cutting- How it Works? Cont.
This will ignite and burn the metal as well as carry away the slag or oxidized residue.
Oxy-fuel cutting can be applied to plain carbon steels, low-alloy steels and other ferrous metals.
Nonferrous metals, stainless steels and cast iron are not usually cut using oxy-fuel equipment.
Ferrous Metals
Non-Ferrous Metals

## Slide 9: Importance of Torch Cutting
More people use the oxy-fuel cutting torch than any other welding process.
The cutting torch is used by workers in virtually all areas including manufacturing, maintenance, automotive repair, railroad, farming, and more.
It is unfortunately one of the most commonly misused processes.
Most workers know how to light the torch and make a cut, but their cuts are very poor quality and often unsafe.
A good oxy-fuel cut should not only be straight and square, but it should require little or no post-cut cleanup.
Excessive post-cutting cleanup results in extra cost, which is an expense that cannot be justified.

## Slide 10: Getting Started- Inspect the Equipment
Inspect the cone end, coupling nut, and torch head for dirt, dust, oil, grease, or damaged parts. Dirt and dust can be removed with a clean cloth.
CAUTION: If oil, grease or damaged parts are detected, DO NOT USE! Report it to the instructor immediately!

## Slide 11: Inspect the “O”Rings
2. Inspect the cutting attachment cone end for missing or damaged “O” rings. Damaged or missing “O” rings can allow gases to mix and will cause backfires or backflash.

## Slide 12: Inspect the Cutting Tips
Inspect the torch head. The tapered seating surfaces must be in good condition.
If dents, burns or burned seats are present, the seat must be resurfaced.
If the torch is used with a bad seat, backfire or backflash may occur.

## Slide 13: Setting up the Cutting Head
Connect the cutting attachment to the welding torch handle and tighten the coupling nut, using hand pressure only.
Wrench tightening may damage “O” rings and create a faulty seal.
HAND TIGHT ONLY

## Slide 14: Tip Selection
5. Select the required size and type of cutting tip.

## Slide 15: Attaching the Cutting Tip
6. Insert the tip in the cutting attachment head and tighten securely with an open-end wrench.
Wrench Tight Connecting Nut