## Slide 1: Lighting the Torch Cont.
14. Depress the cutting oxygen lever.
Note- if the preheat flame changes slightly to a carburizing flame, continue to depress the cutting oxygen lever and increase the preheat oxygen at the cutting attachment until the preheat flames are neutral again.

## Slide 2: Torch Cutting Precautions
IMPORTANT: Check where molten metal and sparks will fall.
Have fire extinguishers available, remove flammable substances, and check where the oxy-fuel hoses are located before starting to work.
Protective leather boots and gloves should be worn while torch cutting.

## Slide 3: Straight Line Cutting

## Slide 4: Torch Cutting Procedures Straight Line Cutting
15. Hold the cutting attachment or torch comfortably in both hands so one hand stabilizes the cutting tip preheat flames approximately 1/8” from the base metal and the other hand is free to depress the cutting oxygen lever.

## Slide 5: Torch Cutting Procedures Straight Line Cutting Cont.
16. Direct the preheat flame on the spot where the cut is to be started.
Before cutting action can start, the base metal must be preheated to a bright cherry red.
When the red spot appears, depress the cutting oxygen lever slowly.

## Slide 6: Torch Cutting Procedures Straight Line Cutting Cont.
17. When the cut has started, move the torch in the direction you wish to cut.
Note: moving too slowly will allow the cut or kerf to fuse together, and moving too fast will not allow the metal to be preheated and the cut will be lost.

## Slide 7: Torch Cutting Procedures Straight Line Cutting Cont.
18. Continue to depress the cutting oxygen lever past the final edge of the base metal for a good “drop cut.”

## Slide 8: Recommended Procedure for Flame Cutting of Thick Steel Plate
Start to preheat; point tip at angle on edge of plate.
Rotate flame back to upright position – keep the dark inner blue flame 1/8” from metal.
Press oxy valve slowly; as cut starts, rotate tip backward slightly.
Now rotate to upright position without moving tip forward.
Rotate tip more - so tip points slightly in direction of cut.
Advance as fast as good cutting action will permit.
Do not jerk; maintain slight leading angle toward cut direction
Slow down; let cutting stream sever corner edge at bottom.
Continue steady forward motion until tip has cleared end.

## Slide 9: Torch Cutting Procedure Piercing a Hole
19. To pierce metal, again hold the cutting attachment or torch comfortably in both hands with one hand stabilizing the cutting tip preheat flames approximately 1/8” from the base metal while the other hand is free to depress the cutting oxygen lever.